医院用窗帘要采用BS 5867-2标准哪种测试方法？

医院作为高安全要求的公共场所，其窗帘需具备严格的防火性能以降低火灾风险。根据英国标准BS 5867-2，医院用窗帘必须采用Type C测试方法，这是该标准中对防火性能要求最严苛的等级。

BS 5867-2 Type C测试的核心要求

- 高频率清洁预处理：需按照BS EN ISO 10528标准进行50次工业水洗循环，模拟长期使用中的磨损和清洁影响。

- 多阶段点火测试：根据BS EN ISO 15025:2002，对垂直悬挂的窗帘样本依次施加5秒、15秒、20秒和30秒的火焰，逐步增加火源强度以验证耐火极限

测试方法与评估标准

- 火焰施加方式：火焰作用于窗帘表面（非边缘），模拟实际火源接触场景

- 通过条件：

火焰及余辉在移开火源后2.5秒内熄灭；

火焰未蔓延至织物边缘；

无燃烧碎片脱落

BS 5867-2基于应用场景的风险分级，定义了Type A（低风险）、Type B（中风险）及Type C（高风险）三种测试方法。以下这三种测试方法的差异对比：

| 测试类型 | 适用场景 | 预处理要求 | 点火时间 |
| --- | --- | --- | --- |
| Type A | 低风险区域 | 12次水洗或6次干洗 | 10秒 |
| Type B | 酒店、办公室 | 清洁前后测试 | 15秒 |
| Type C | 医院、疗养院 | 50次水洗 | 5-30秒分阶段 |

Type A 判定依据（10秒）：

任何燃烧孔的任何部分不可达到样品的任一垂直边

火焰最低边界的任何部分均不可到达样品的任一垂直边

不可以烧断第一个标记线

Type B 判定依据（15秒）：

任何燃烧孔的任何部分不可达到样品的任一垂直边

火焰最低边界的任何部分均不可到达样品的任一垂直边

Which test method of BS 5867-2 should be used for hospital curtains?

As a public place with high safety requirements, the curtains in hospitals must have strict fire resistance to reduce the risk of fire. According to the British standard BS 5867-2, hospital curtains must adopt the Type C test method, which is the most stringent level of fire resistance in the standard.

Core requirements of BS 5867-2 Type C test

 High frequency cleaning pre-treatment: 50 industrial water washing cycles are required in accordance with BS EN ISO 10528 standard to simulate the wear and cleaning effects of long-term use.

 Multi-stage ignition test: According to BS EN ISO 15025:2002, the vertically hung curtain samples are subjected to 5 seconds, 15 seconds, 20 seconds and 30 seconds of flame in sequence, and the intensity of the fire source is gradually increased to verify the fire resistance limit

Test method and evaluation criteria

Flame application method: The flame acts on the curtain surface (not the edge) to simulate the actual fire source contact scene

Passing conditions:

The flame and afterglow are extinguished within 2.5 seconds after the fire source is removed;

The flame does not spread to the edge of the fabric;

No burning fragments fall off

BS 5867-2 defines three test methods based on the risk classification of application scenarios: Type A (low risk), Type B (medium risk) and Type C (high risk). The following is a comparison of the differences between these three test methods

Type A judgment basis (10 seconds):

Any part of any burning hole cannot reach any vertical side of the sample

Any part of the lowest edge of the flame cannot reach any vertical side of the sample

The first marking line cannot be burned

Type B judgment basis (15 seconds):

No part of any burning hole can reach any vertical edge of the sample

No part of the lowest edge of the flame can reach any vertical edge of the sample